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LB668 acidic silicone sealant
1、Product Features
A silicone sealant designed specifically for point glass curtain walls, full glass curtain walls, glass skylights, other large glass bonding seals, and fish tank bonding seals, with single component, medium high modulus, and acid curing properties. It has excellent structural bonding performance and weather aging resistance. After manual accelerated weather aging testing, the various physical and chemical properties of the sealant have not changed significantly. The product can crosslink and form a permanent elastomer at room temperature.
2、Product Application
Structural bonding and sealing for curtain wall engineering, including assembly between glass and metal materials in factory or on-site construction; bonding and sealing of insulating glass; and numerous other architectural and industrial applications.
3、Technical Specifications
	parameter
	numerical value
	execution standard

	appearance
	paste
	

	Surface drying time，min
	8
	GB/T 13477

	extrudability，ml/min
	180
	GB/T 13477

	Construction time，min
	5-8
	

	sag
	vertical
	0
	GB/T 13477

	
	level
	0
	

	hardness，Shore A
	26
	GB/T 531

	Tensile bonding strength / MPa
	23℃
	0.65
	GB/T 13477

	
	90℃
	0.51
	

	
	－30℃
	0.72
	

	
	UV aging of water
	0.50
	

	tensile bond strength %
	无破坏
	GB/T 13477

	Thermogravimetric %
	2
	GB 16776


4、Meet the standard
SR 2MG AK JC/T 485-2007
5、Usage restrictions
All materials that may leak oil, plasticizers, or solvents, such as the surface of oil soaked wood, oil bottom steel plate joints, and some uncured or partially vulcanized rubber pad materials and tapes in poorly ventilated places, because silicone sealant needs to absorb moisture from the air to solidify; Frosty or damp surfaces, areas that are continuously submerged in water, or areas that are constantly damp throughout the year; The paint surface may fail to seal and bond due to paint peeling or cracking; When the surface temperature of the material is below 4 ℃ or above 40 ℃, it is not suitable for construction.
6、Packaging
   300ml plastic drum packaging .
7、Color
   transparent ,Black, gray, white or other colors requested by the user
8、Shelf life
   Store in a cool and dry place below 27 ℃, with a shelf life of 12 months from the date of production.
9、Technical Service
   a、Provide complete technical documentation.
   b、Adhesive testing:
    The LB silicone sealant series products have excellent adhesion to most building materials, such as glass, anodized aluminum, tiles, granite, bricks, wood, steel, and most plastics. But due to the continuous emergence of new building materials and the application of new surface treatment technologies; We cannot guarantee that the sealant is suitable for all materials, and in some cases, it is necessary to conduct adhesion tests between the sealant and the materials used in the project. Our laboratory can conduct adhesion testing for customers, evaluate the bonding performance between our sealant products and the materials selected for customer engineering, and submit the experimental results, product recommendations, surface cleaning methods, and whether to use primer in writing to customers.
10、Safety Instructions
    This product is non-toxic after complete curing, but should be avoided from contact with eyes before curing. If it comes into contact with eyes, please rinse with plenty of water and seek medical attention; Uncured products should be avoided from contact with children. This product will release ketoxime substances during the curing process. Ventilation should be taken into account in the construction and curing areas to avoid adverse effects on people caused by excessive concentration of ketoxime substances.
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