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  LB888 neutral silicone anti mold sealant
1、Product Features
Single component, neutral curing, silicone sealant specially designed for various anti mold requirements (such as sealing in kitchens and bathrooms). Has excellent anti mold performance, tested according to GB/T 1741 and ASTM G 21 methods, with an anti mold grade of 0, especially suitable for sealing joints in environments prone to mold growth. When in use, use a glue gun to squeeze the sealant from the packaging tube into the seam that needs to be sealed. The sealant reacts with the moisture in the air at room temperature and solidifies to form a weather resistant and elastic silicone sealant.
2、Product Application
Installation and waterproof, anti mold sealing of various kitchen utensils and sanitary ware; Many other buildings and industrial uses.
3、Technical Specifications
	parameter
	numerical value
	execution standard

	appearance
	paste
	

	Surface drying time，h
	≤3
	GB/T 13477

	Construction time，min
	10-20
	GB/T 13477

	Sag，mm
	vertical
	0
	GB/T 13477

	
	level
	0
	

	hardness，Shore A
	42
	GB/T 531

	tensile modulus/MPa
	23℃
	0.52
	JC/T 885

	
	-20℃
	/
	

	Tensile adhesion
	No destruction
	GB/T 13477

	Adhesive properties after hot pressing and cold drawing
	No destruction
	JC/T 885

	Fixed tensile adhesion after immersion in water
	No destruction
	JC/T 885

	Thermogravimetric %
	2
	GB 16776

	Mold resistance
	0
	GB/T 1741


4、Meet the standard
SR-12.5E-0-JC/T885-2001

5、Usage restrictions
All materials that may leak oil, plasticizers, or solvents, such as the surface of oil soaked wood, oil bottom steel plate joints, and some uncured or partially vulcanized rubber pad materials and tapes in poorly ventilated places, because silicone sealant needs to absorb moisture from the air to solidify; Frosty or damp surfaces, areas that are continuously submerged in water, or areas that are constantly damp throughout the year; The paint surface may fail to seal and bond due to paint peeling or cracking; When the surface temperature of the material is below 4 ℃ or above 40 ℃, it is not suitable for construction.
6、Packaging
   300ml plastic drum packaging .
7、Color
   Black, gray, white or other colors requested by the user
8、Shelf life
   Store in a cool and dry place below 27 ℃, with a shelf life of 12 months from the date of production.
9、Technical Service
   a、Provide complete technical documentation.
   b、Adhesive testing:
    The LB silicone sealant series products have excellent adhesion to most building materials, such as glass, anodized aluminum, tiles, granite, bricks, wood, steel, and most plastics. But due to the continuous emergence of new building materials and the application of new surface treatment technologies; We cannot guarantee that the sealant is suitable for all materials, and in some cases, it is necessary to conduct adhesion tests between the sealant and the materials used in the project. Our laboratory can conduct adhesion testing for customers, evaluate the bonding performance between our sealant products and the materials selected for customer engineering, and submit the experimental results, product recommendations, surface cleaning methods, and whether to use primer in writing to customers.
  c、Compatibility testing:
     If the auxiliary materials for assembly such as foam strips and double-sided adhesive strips are incompatible with silicone rubber, the silicone rubber will change color or even lose its cohesiveness. To avoid such problems, our laboratory provides compatibility testing services to customers. Customers can send us the auxiliary materials selected in the project by mail (or in other forms), and our laboratory will conduct compatibility testing and provide a written test report.
10、Interface Design
Please refer to the "Guidelines for the Use of LB Silicone Building Sealants".
11、Safety Instructions
    This product is non-toxic after complete curing, but should be avoided from contact with eyes before curing. If it comes into contact with eyes, please rinse with plenty of water and seek medical attention; Uncured products should be avoided from contact with children. This product will release ketoxime substances during the curing process. Ventilation should be taken into account in the construction and curing areas to avoid adverse effects on people caused by excessive concentration of ketoxime substances.
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