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 LB798 neutral silicone weather resistant sealant
1、Product Features
Single component, neutral curing, silicone sealant specially designed for weather resistant sealing of various curtain walls (glass curtain walls, aluminum curtain walls, etc.), various door and window projects, etc., with excellent weather resistance performance. When in use, use a glue gun to squeeze the sealant from the packaging into the seam that needs to be sealed. The sealant reacts with moisture in the air at room temperature and solidifies to form a weather resistant and elastic silicone sealant.
2、Product Application
Weather resistant sealing of various glass curtain walls, sealing of joints in concrete, plastic, and metal, and sealing of joints in roof buildings; Installation and sealing of various door and window projects; Many other buildings and industrial uses.
3、Technical Specifications
	parameter
	numerical value
	execution standard

	appearance
	paste
	

	Surface drying time，h
	≤3
	GB/T 13477

	extrudability，ml/min
	≥150
	GB/T 13477

	displacement capacity，%
	±25
	

	Sag，mm
	≤3
	GB/T 13477

	elastic recovery rate，%
	≥80
	GB/T 14683

	Fixed tensile adhesion after immersion in water
	No destruction
	GB/T 14683

	Adhesive properties after hot pressing and cold drawing
	No destruction
	GB/T 14683

	Adhesive properties after UV irradiation
	No destruction
	GB/T 14683

	Adhesion after immersion in water and exposure to light
	No destruction
	GB/T 14683

	Thermogravimetric %
	3
	GB 16776


4、Meet the standard
SR GB/T 14683-I-Gn-25HM ，ISO11600-G-25HM，ASTM C 920 25HM
5、Usage restrictions
All materials that may leak oil, plasticizers, or solvents, such as the surface of oil soaked wood, oil bottom steel plate joints, and some uncured or partially vulcanized rubber pad materials and tapes in poorly ventilated places, because silicone sealant needs to absorb moisture from the air to solidify; Frosty or damp surfaces, areas that are continuously submerged in water, or areas that are constantly damp throughout the year; The paint surface may fail to seal and bond due to paint peeling or cracking; When the surface temperature of the material is below 4 ℃ or above 40 ℃, it is not suitable for construction.
6、Packaging
   300ml plastic drum packaging or 500ml, 590ml composite film flexible packaging.
7、Color
   Black, gray, white or other colors requested by the user
8、Shelf life
   Store in a cool and dry place below 27 ℃, with a shelf life of 12 months from the date of production.
9、Technical Service
   a、Provide complete technical documentation.
   b、Adhesive testing:
    The LB silicone sealant series products have excellent adhesion to most building materials, such as glass, anodized aluminum, tiles, granite, bricks, wood, steel, and most plastics. But due to the continuous emergence of new building materials and the application of new surface treatment technologies; We cannot guarantee that the sealant is suitable for all materials, and in some cases, it is necessary to conduct adhesion tests between the sealant and the materials used in the project. Our laboratory can conduct adhesion testing for customers, evaluate the bonding performance between our sealant products and the materials selected for customer engineering, and submit the experimental results, product recommendations, surface cleaning methods, and whether to use primer in writing to customers.
  c、Compatibility testing:
     If the auxiliary materials for assembly such as foam strips and double-sided adhesive strips are incompatible with silicone rubber, the silicone rubber will change color or even lose its cohesiveness. To avoid such problems, our laboratory provides compatibility testing services to customers. Customers can send us the auxiliary materials selected in the project by mail (or in other forms), and our laboratory will conduct compatibility testing and provide a written test report.
10、Interface Design
Please refer to the "Guidelines for the Use of LB Silicone Building Sealants".
11、Safety Instructions
    This product is non-toxic after complete curing, but should be avoided from contact with eyes before curing. If it comes into contact with eyes, please rinse with plenty of water and seek medical attention; Uncured products should be avoided from contact with children. This product will release ketoxime substances during the curing process. Ventilation should be taken into account in the construction and curing areas to avoid adverse effects on people caused by excessive concentration of ketoxime substances.
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